Digital Barcol Impressor   DBI-1

Product Description

DBI-1,  a digital  indentation   hardness   tester,  is the latest  design  and  development   of our company.  It is  characterized   in that

provided  with  a balance  positioning,   a digital   display  of hardness  value,  and  a non disassembly   calibration   and  adjusting.

It  is with good  stability,   convenient  calibration,    and high  accuracy  of detection.   It is mainly  used  in aluminum   processing  industry,

testing  pure  aluminum,  soft  aluminum,   thick aluminum   alloy, aluminum   strip,  aluminum  rod,  aluminum  castings,   aluminum

forgings  and  aluminum  alloy  products.  Also,  it can  be used  for glass  steel  industry.

The relevant   standard  is ASTM  B648-00,

ASTM HD2583-07,   and  GB / T 3854-2005.

Applications fields:  
*Aluminum     *Aluminum Alloys    *Soft Metals   *Composite Materials  *Glass Steel

Product Features

* Small  in size,  portable.  Single  hand  operation,   easy to  use. Can

be used  in any occasion   as long  as the hand  can reach.

* Wide  test range,  can test  from  very soft  pure aluminum   to a

particularly   hard  aluminum  alloy.  effective  test  range  equivalent

to the Brinell   Hardness  of 25~150HB.

* No need  to  be supported.   Just test  on one  side of the  sample

with the  hardness  tester,  no need  to be supported.   It is  suitable

for the  test of large  and  extra thick  workpiece.

* With the  maximum  hold  function,  recording   the maximum

hardness  value  during  measurements.

* Can be  used for  measuring  Barcol  Hardness,   other  hardness

value  can be calculated   out  by the experimental   curve.  Such  as

Brinell  Hardness   (HB), Vickers  Hardness   (HV),  Webster

Hardness  (HW),  Rockwell  Hardness   (HRB/HRE/HRF/HRH).

Product Parameters

Barcol  Hardness  (Hba)

other  hardness  value  can be  calculated  out  by the experimental    curve

Parameters

Measurement   Range

Resolution

0~100  HBa, equivalent   to the  Brinell  hardness  of  25~150HB

0.1 HBa

81~88  HBa±1  HBa

42~48  Hba±2  HBa

81~88  HBa±1.5  HBa

42~48  HBa±2.5  Hba

Temperature:   0~50°C

Humidity:   <80%RH

Indication   Error

Repeatability   Error

Operating   Condition

Size

170x63x82   mm

Power  Supply

2x1.5vAAA  Um-4  Battery

Weight

390g  (Not Including   Batteries)

Product   Accessories

Standard  Accessories

Optional  Accessories

Main  Unit, 2 Pins,  2 Standard  Blocks,   Pin Length  Calibration   Block,

Screw  Driver,  Spanner,  Carrying  Case,  Operation   Manual

Bluetooth  data  output

www.capitalinstrument.com